## Slide 1
V-2201 Integrity Briefing
Sovereign AI Engineering Workbench | 2026-09-13 15:24 UTC

## Slide 2
Statutory Integrity Briefing
Automated compliance evaluation prepared by Sovereign On-Premise Agentic AI Workbench (SIH26117). Operating under 100% offline, air-gapped refinery deployment.

## Slide 3
Ultrasonic Survey & Thickness Status
• Equipment ID: V-2201 (Knockout Drum) • Design Pressure: 10.5 kg/cm²g | Design Temperature: 120°C • Nominal Shell Thickness: 12.0 mm | Minimum Measured Shell: 11.2 mm • Maximum Corrosion Loss: 0.80 mm (6.7% of initial wall thickness) • Remaining Corrosion Allowance: 78% on critical bottom shell course

## Slide 4
ASME / API 510 Verification Trace
• Governing Formula: t_min = (P × R) / (S × E − 0.6 × P) • Variable substitution: E = 0.85, P = 10.5, R = 600.0, S = 1380.0 • 10.5 × 600 = 6300 • 1380 × 0.85 = 1173 • 0.6 × 10.5 = 6.3 • Calculated t_min: 5.3998 mm • Actual Measured: 11.2 mm • Safety Margin: +5.80 mm excess wall thickness over statutory limit

## Slide 5
Statutory Recommendation & Sign-Off Gate
• Inspector Recommendation: Approved for continued service until next cycle (5 years). • Next Statutory Inspection Due: September 2031 per Factories Act / OISD-130. • Mandatory Action: Human Engineer Authorization required prior to turnaround closure.